JHE CARBONLESS PAPER SPECIFICATIONS

| Grades: | Blue Images | Black Images | Test Methor |
| --- | --- | --- | --- |
| Regular basis weights (gsm): | CB white: 45, 50, 55 CB tinted: 55; CFB white or tinted: 50, 52, CF white or tinted; 47, 55 GSM not mentioned herein can be produced subject to our Min. Order requirement. | CB white: 45, 50, 55 CFB white or tinted: 50, 52 CF white or tinted; 47, 55 GSM not mentioned herein can be produced subject to our Min. Order requirement. | GB451.2 |
| Basis Weight variation: | ±5%; | ±5%; | Internal Method |
| Caliper Variation (CD): | ≤5μm for 50GSM or less GSM; ≤7µm for 50GSM or greater GSM | ≤5μm for 50GSM or less GSM; ≤7µm for 50GSM or greater GSM | Internal Method |
| Paper Density: | 0.70-0.85 g/cm3; | 0.70-0.85 g/cm3; | GB451.3 |
| Opacity: | ≥65%; | ≥65%; | GB1543 |
| Smoothness (CF side): | ≥60 s; | ≥60 s; | GB456 |
| Whiteness: | ≥85% with OBA; ≥78% without OBA; | ≥85% with OBA; ≥78% without OBA; | GB7974 |
| Chromatic deviation: | ≤2.0% (coated side for tinted grades); | ≤2.0% (coated side for tinted grades); |  |
| Curls: | ≤12 mm | ≤12 mm | GB/T13528 |
| Optical densityΔD (5min): | ≥0.70 CB rolls and sheets, 3 ply prints; ≥0.75 CFB rolls, 5 ply prints; ≥0.75 CFB sheets, 5 ply prints; ≥0.80 CF, 5 ply prints; | ≥0.30 (3 ply prints) | Internal Method |
| Imaging Sensitivity (3 ply prints): | ΔE≥88%;ΔD≥88%; | ΔE≥88%;ΔD≥88% (3 ply prints); | Internal Method |
| Surface strength (medium viscosity printing ink): | ≥0.5 m/s (printing side); | ≥0.5 m/s (printing side); | Internal Method |
| Light resistance (residual ΔE after 144 hrs): | ≥50%; | ≥50%; | Internal Method |
| Friction resistance (ΔE): | ≤5%; | ≤5%; | Internal Method |
| TSI (MD): | ≥60 N.m/g; | ≥60 N.m/g; | Internal Method |
| Surface PH: | 6.0-9.0 | 6.0-9.0 |  |
| Moisture on delivery: | ≤8.0% CB and CFB sheets; 6.0%-7.5 % CB and CFB rolls; 6.5%-8.0% CF; | ≤8.0% CB and CFB sheets; 6.0%-7.5 % CB and CFB rolls; 5.0%-7.5% CF; | GB462 |
| Regular roll sizes: | 120-600mm, paper length = 6,000m or 12,000m but 6,000m is highly recommended. |
| Regular sheet sizes: | 700*1000, 610*914, 690*890, 610*860, 770*1100; 720*920, etc |
| Export Packing: | Wrapped inside with thin plastic film against moisture, and outside with heavy craft paper for sheets, corrugated paperboard for rolls. |